## Slide 1: Implementation of Soil Carbonation for Subgrade Stabilization
Manifold for CO2 Gas cylinders
Gas mass flow meter
SK Belal Hossen, EI1, Aaron P. Gallant, PhD, PE2 and Warda Ashraf, PhD3
1Graduate student, Civil and Environmental Engineering, University of Maine, Orono, Maine, USA. e-mail: sk.hossen@maine.edu; 2Assistant Professor, Civil and Environmental Engineering, University of Maine, Orono, Maine USA. e-mail: aaron.gallant@maine.edu;
3Assistant Professor, Department of Civil Engineering, Center for Advanced Construction Materials (CACM), University of Texas at Arlington, Texas, USA. e-mail: warda.ashraf@uta.edu
2. Field investigation- instrumentation and testing
1. Motivation/Background
Soil carbonation
Potential benefits
Untreated soils
Ca2+ + CO32- = CaCO3
Carbonation
Cementation in soils
Ca(OH)2 [s]+ H2O [l] + CO2[g] CaCO3 [s] (↓) +2H2O[l]
Step 1
Step 2
Objective
Testing
Note: s=solid, l=liquid, g=gas, ↓=deposited
2021 TIDC Annual Student Poster Competition
Funding for this research is provided by the Transportation Infrastructure Durability Center at the University of Maine under grant 69A3551847101 from the U.S. Department of Transportation’s University Transportation Centers Program.
Utilize and store CO2 gas into subgrade soils→ more sustainable and environmentally friendly
Relatively faster strength improvement→ reducing construction time and/or construction costs
Performance of soil carbonation on the laboratory scale
Effective means to introduce the gaseous CO2 into subgrade soils with optimum performance (in terms of maximum binder formation with minimal gas loss and strength improvement)
Fig 7.) Binder content measurement
Fig 6.) Field CBR testing setup
Fig 4.) Soil box preparation
Fig 2.) Relationship between UCS and binder content of carbonated sand mixed with 10% lime
Mixing
Box preparation in layers
Compaction
After completion
Fig 3.) Carbonation in the box
a.) Bender Element (BE)
b.) installation in the soil box
Fig 5.) Shear wave measurement
October 28, 2021
Fig 1.) Reaction mechanism for soil strength improvement
CO 2 Gas
Soil box (2 m in length, 1 m in width and 0.75 m in height)